## Slide 1: Integrated Computational Materials Engineering (ICME)
John Allison
University of Michigan
ICME Short Course
June 8, 2017

## Slide 2
50
100
150
200
250
0
1
10
100
Al-4Cu
Al-4Cu-0.05Sn
Al-4Cu-0.3Mg
Al-4Cu-0.3Mg-0.5Si
Al-4Cu-0.3Mg-0.4Ag
Al-4Cu-0.3Mg-0.4Ag-1Li
200°C
Hardness (VHN)
Ageing Time (h)
Courtesy of J. F. Nie

## Slide 3: It takes 10-20 years to develop a new material
50
100
150
200
250
0
1
10
100
Al-4Cu
Al-4Cu-0.05Sn
Al-4Cu-0.3Mg
Al-4Cu-0.3Mg-0.5Si
Al-4Cu-0.3Mg-0.4Ag
Al-4Cu-0.3Mg-0.4Ag-1Li
200°C
Hardness (VHN)
Ageing Time (h)
1906
1989
Societal and global competitiveness requires us to do this faster and cheaper!
Courtesy of J. F. Nie

## Slide 4: Materials Genome Initiative
. . . This initiative offers a unique opportunity for the United States to discover, develop, manufacture, and deploy advanced materials at least twice as fast as possible today, at a fraction of the cost.
President Barack Obama, 24 June 2011
Announcing the Materials Genome Initiative
“(In this context) genome connotes a fundamental building block toward a larger purpose” NSTC MGI White Paper, 2011

## Slide 5: Outline
Integrated Computational Materials Engineering (ICME) – What it is and why it’s important
Virtual Aluminum Castings – An ICME Case Study at Ford
ICME – The Next Big Thing in Structural Materials and An Essential Element of MGI
Thoughts on ICME for Integrated Computational Materials Education (ICME for ICME)

## Slide 6: ICME/MGI Historical Highlights
1989
DOE: Advanced Strategic Computing Initiative
NRC: Materials Science & Eng for the 1990s
1995
NRC: The Valley of Death
1999
DARPA-AIM
AFOSR-MEANS
2001
2004
2010
2008
NRC-ICME
2011
ONR-D3D
2009
WTEC-SBES
BES-ASCR
We are at a tipping point!
European Union
Virtual Aluminum Castings

## Slide 7: Materials Genome Initiative
. . . This initiative offers a unique opportunity for the United States to discover, develop, manufacture, and deploy advanced materials at least twice as fast as possible today, at a fraction of the cost.
President Barack Obama, 24 June 2011
Announcing the Materials Genome Initiative
“(In this context) genome connotes a fundamental building block toward a larger purpose” NSTC MGI White Paper, 2011

## Slide 8: Materials Genome Initiative
Coordinated Multi-agency effort – DOE, DOD, NSF, NIST with White House OSTP leadership
$150M / year “10 year program”
Essential ingredients
  Collaboration
  Integration of theory,
    simulation and experiments
  Information Infrastructure
  Workforce development
  ICME
These represent important building blocks for ICME

## Slide 9: A Well-Equipped Workforce (Excerpt from 6/2014 MGI Strategic Plan)
… the next generation of materials scientists and engineers must be able to expertly use these tools to achieve the success promised by MGI….
.. before the future generation workforce can be equipped to take advantage of the Materials Innovation Infrastructure, instructors must first be provided information on these new tools, research approaches, and their value.

## Slide 10: US National Materials Advisory Board - Committee on Integrated Computational Materials Engineering (ICME) Tresa Pollock, Chair John Allison, Vice Chair 2008 Free Download: http://books.nap.edu/catalog/12199/
Notes: 10

## Slide 11
11
The Vision
Computationally-driven materials development is a core activity of materials professionals in the upcoming decades, uniting materials science with materials engineering and integrating materials more holistically and computationally with product development.
Notes: 11

## Slide 12: Integrated Computational Materials Engineering (ICME) is the integration of materials information, captured in computational tools, with engineering product performance analysis and manufacturing-process simulation.*
* NAE ICME Report, 2008
What is ICME?
Quantitative
Structure-Property Relations
Quantitative
Processing-Structure Relations
Chemistry
Thermodynamics
Diffusion
Manufacturing
Process
Simulation
Engineering Product Performance Analysis
Constitutive Models
Process & product optimization
Innovation

## Slide 13: Integrated Computational Materials Engineering (ICME) is the integration of materials information, captured in computational tools, with engineering product performance analysis and manufacturing-process simulation.*
* NAE ICME Report, 2008
What is ICME?
Manufacturing
Process
Simulation
Process & product optimization
Innovation
Microstructure
Distribution
Property Distribution
Product Performance Analysis

## Slide 14
Using advanced computational techniques, designs can be studied and optimized in matters of hours or days. Optimization of new materials must be done experimentally and can take 10-20 years.
Shape optimization of hypersonic vehicles
Source: K. Bowcutt, Boeing

## Slide 15: Why this is important
Innovations in materials and tight coupling of component design, materials and manufacturing have been key sources of industrial competitiveness
These innovations and tight coupling are threatened by advances in computational capability in design and manufacturing that have “left materials field in the dust”.
The global economy requires efficient engineering, manufacturing and R&D

## Slide 16: The Divide Separating Materials Science and Materials Engineering
Quantum Mechanics
Theory
Kinetics Experiment
Thermal Growth
g
Calculated
Phase Diagram
Predicted Volume Change

## Slide 17: Integrated Computational Materials Engineering provides a means to link:
  Science and Engineering
  Manufacturing, Materials and Design
  Experiments, Theory, Simulation
  Information Across Disciplines
8

## Slide 18
Ford Virtual Aluminum Castings

## Slide 19
ABAQUS
Initial
Geometry
Database of
Material
Properties
Traditional Durability Analysis
Predict
Service
Life
Load
Inputs
Durable
Component
Y
N

## Slide 20
ABAQUS
Initial
Geometry
Database of
Material
Properties
Traditional Durability &
Manufacturing Analysis
Predict
Service
Life
Load
Inputs
Durable
Component
Y
N
N
Model
Casting
Ensure
Castability
Y
MagmaSOFT/ ProCast

## Slide 21
ABAQUS
Initial
Geometry
Database of
Material
Properties
Traditional Product Development Process
Predict
Service
Life
Load
Inputs
Durable
Component
Y
N
N
Model
Casting
Ensure
Castability
Y
ProCAST/MagmaSOFT
Build, Test,
Re-Build,
Re-Test

## Slide 22
Predict
Local
Micro-
structure
Predict
Service
Life
Load
Inputs
Optimized
Component
Meet Property
Requirements
N
Y
Optimized
Process &
Product
Y
N
MagmaSOFT/ ProCAST
ABAQUS
Product and Process
Predict
Residual
Stress
Predict
Local
Properties
Model
Casting
and Heat
Treatment
Product
Property
Requirements
Product
Property
Requirements
Initial
Geometry
Alloy
Composition
Ensure
Castability
Y
N
Rearrange the Production Simulations

## Slide 23
Predict
Local
Micro-
structure
Predict
Service
Life
Load
Inputs
Optimized
Component
Meet Property
Requirements
N
Y
Optimized
Process &
Product
Y
N
MagmaSOFT / ProCAST
ABAQUS
Product and Process
Predict
Residual
Stress
Predict
Local
Properties
Model
Casting
and Heat
Treatment
Product
Property
Requirements
Product
Property
Requirements
Initial
Geometry
Alloy
Composition
Ensure
Castability
Y
N
Virtual Aluminum Castings
The Ford Experiment in ICME

## Slide 24: Materials Engineering is all about compromises – ICME provides a means to conduct quantitative tradeoffs
Casting
Precipitation
Micro porosity
Eutectic Phases
Chemistry
Thermodynamics/
Kiinetics
n
Solution Treatment
Aging
Heat Treatment
Processing
Microstructure
Properties
High Cycle Fatigue
Low Cycle Fatigue
Yield Strength
Thermal Growth
Cast Aluminum Processing-Structure-Property Linkages

## Slide 25
1 m
Engine Block
1 – 10 mm
Macrostructure
Grains
Macroporosity
Properties
• High cycle fatigue
• Ductility
10 – 500um
Microstructure
Eutectic Phases
Dendrites
Microporosity
Intermetallics
Properties
• Yield strength
• Tensile strength
• High cycle fatigue
• Low cycle fatigue
Thermal Growth
• Ductility
1-100 nm
Nanostructure
Precipitates
Properties
• Yield strength
Thermal Growth
• Tensile strength
• Low cycle fatigue
• Ductility
0.1-1 nm
Atomic Structure
Crystal Structure
Interface Structure
Properties
• Thermal Growth
Yield Strength
Key metallurgical processes occur at many length scales – and all can be influenced by manufacturing history

## Slide 26
1 m
Cast Aluminum
Engine Block
1 – 10 mm
10 – 500mm
0.1-1 nm
Microstructures
0.1-.3nm
1-100 nm

## Slide 27: q’ Al2Cu Precipitates
Li, Zhang, Chen, Allison

## Slide 28: Physics Based Models – Yield Strength
Yield strength (sY) is the sum of an intrinsic strength (si), a precipitation hardening strength (sppt), and a solid solution strength (sss):
Zhu & Starke, 1999
f = volume fraction of theta’
d = diameter of theta’ platelet
w= thickness of theta’ platelet

## Slide 29
Temperature, oC
Mole Fraction Cu
Al
q-phase
q’-phase
Liquid
(Al)
First-Principles Modification of Al-Cu Phase Diagram Incorporating Metastable
q’-phase
Metastable states just as easy to calculate as stable states
Notes: 29

## Slide 30
TEM Characterization of Precipitate Morphology vs Aging Time
(319 Al alloy with 3, 3.5 and 4%Cu)
VAC models capture experimental understanding
where robust physics-based models are not available

## Slide 31: Aging Response of 319 Aluminum Prediction vs. Experimental

## Slide 32
Microstructure (Al2Cu)
Micromodel (ThermoCALC)
Empirical Kinetics (OPTCAST)
Initial Geometry
CAD Geometry
and Mesh
Filling
Accurate filling Profile (OptCast)
Thermal Analysis
Boundary Conditions (OPTCAST)
Fraction solid Curves (ThermoCALC)
Yield Strength
Aging Model
(ThermoCALC)
Virtual Aluminum Castings Process Flow
Local Yield Strength Prediction

## Slide 33: Model Validation & Accuracy
Normal Production Region

## Slide 34: Using Virtual Aluminum Castings in Product and Process Optimization
Aging temperature 240C for 5hrs
210
230
205
Aging at 250C for 3hrs
Optimized Heat Treatment Process
Faster and Stronger !!
220
Initial Heat Treatment
Process
Target Strength = 220 MPa

## Slide 35
Initial Geometry
Filling Analysis
Thermal Analysis
Local Porosity
Local Fatigue Strength
Local Fatigue Strength Prediction

## Slide 36
Prediction of Local Fatigue Strength
Pore Size (Microns)
Micro Porosity
1200 Microns
500 Microns
200 Microns
MPa
Fatigue Strength
56 MPa
67 MPa
80+ MPa

## Slide 37: Use of ICME For New Process Development and Selection
Local Fatigue Strength
84MPa
56MPa
Gravity Casting
Low Pressure Casting
VAC enabled an unprecedented acceleration in the time for process development and selection

## Slide 38
Virtual Aluminum Castings
Local Residual Stresses
Local Fatigue Properties
Component Durability
Linking Manufacturing, Materials and Design
Component Durability

## Slide 39: ICME enables materials to be part of the design optimization process
Example: Advanced Exhaust Manifold Design (800-900°C)
Solution 1:
New Cast Steel Alloy Design
Integration of exhaust manifold into cast aluminum cylinder head
Solution 2: Use Ford Virtual Aluminum Castings
VAC enabled an unprecedented acceleration in the time for new component design and virtual manufacture and testing

## Slide 40
Predict
Local
Micro-
structure
Predict
Service
Life
Load
Inputs
Optimized
Component
Meet Property
Requirements
N
Y
Optimized
Process &
Product
Y
N
ProCAST/MagmaSOFT
ABAQUS
Product and Process
Predict
Residual
Stress
Predict
Local
Properties
Model
Casting
and Heat
Treatment
Product
Property
Requirements
Product
Property
Requirements
Initial
Geometry
Alloy
Composition
Ensure
Castability
Y
N
Virtual Aluminum Castings (VAC)

## Slide 41
Targets
The VAC Business Case
IMPROVE TIMING: Reduce product
and process development time 15-25%
IMPROVE QUALITY:
  Improve launch quality /reduce scrap
  Eliminate failures during product development
  Ensure high mileage durability
IMPROVE PERFORMANCE:
  Enable high performance heads & blocks
  Reduce weight of components
REDUCE COST:
  Cost reduction/avoidance over $120M
GLOBAL USERS
  North American Powertrain Operations
  European Powertrain Ops
  Ford of Asia-Pacific (China &
    Australia)
  Mazda
  (Volvo/Jaguar)

## Slide 42: VAC Modeling Methods
Ab Initio / First Principles Theory (VASP etal)
Phase Field Models
Thermodynamic Equilibria & Diffusion (ThermoCalc, Pandat & Dictra)
Phenomenological micromodels for microstructural evolution & mechanical properties
Continuum mechanics models
  Micromechanics
  Constituitive models (State Variable and Classical Plasticity)
  Crystal Plasticity (FEM)
Optimization Techniques (DOT, iSight)
Manufacturing Simulation Software
  Fluid Flow – CFD (Fluent, ProCast, MagmaSoft)
  Solidification (MagmaSoft, ProCast)
  Thermal analysis (MagmaSoft, ProCast, Abaqus)
  Stress Analysis (Abaqus)

## Slide 43
Former Team Members
  John Allison
  Ruijie Zhang
  Nagendra Palle
  Chris Wolverton (NW)
  Bill Donlon
  Ravi Vijayraghavan
  Don Siegel (UofM)
Ford R&A VAC Team
  John Allison
  Mei Li
  XuMing Su
  Larry Godlewski
  Carlos Engler
  Bob Frisch
  Joy Hines Forsmark
  John Lasecki
  Jake Zindel
  Eben Prabhu
  Richard Chen
Ford VAC R&D Team

## Slide 44
Ford VAC - University Partners
University of Michigan – Prof. Wayne Jones
  Aging models of Aluminum Alloys
  Porosity-fatigue models for 319 Al
  Ultrasonic fatigue (NSF)
Imperial College –Prof. Peter Lee
  Microporosity modeling
Tsinghua University – Prof. Baicheng Liu
  Modeling HPDC processes
Pennsylvania State University – Prof. L. Chen
  Modeling microstructural evolution (NSF)
University of Wisconsin – Prof. A. Chang
  Thermodynamics Models for Cast Al & Mg (SBIR)
Ohio State University – Prof. S. Ghosh
  Modeling Ductility in Cast Al (NSF)
University of Illinois – Prof. H. Sehitoglu/ J. Dantzig
  Modeling Thermal-Mechanical Fatigue of Cast Aluminum
  Prediction of residual stresses/quench cracking in Cast Aluminum
  Optimization Methodologies

## Slide 45: ICME/MGI Historical Highlights
1989
DOE: Advanced Strategic Computing Initiative
NRC: Materials Science & Eng for the 1990s
1995
NRC: The Valley of Death
1999
DARPA-AIM
AFOSR-MEANS
2001
2004
2010
2008
NRC-ICME
2011
ONR-D3D
2009
WTEC-SBES
BES-ASCR
We are at a tipping point!
European Union
Virtual Aluminum Castings

## Slide 46
Early ICME implementations have been successful in a wide variety of industries
Benefits have included more rapid product development, reduced testing costs and more efficient engineering
Return-on-investments in the range of 3:1 to 9:1 have been realized.
Typical investments were in the $5-20M range.
ICME “Case Studies” have
demonstrated the promise
Notes: 46

## Slide 47: Selected Conclusions
Industrial acceptance of ICME is hindered by the slow conversion of science-based materials computational tools to engineering tools and by the scarcity of materials engineers trained to use them.
ICME as a discipline within materials science and engineering does not yet truly exist - ICME is in it’s infancy.
For ICME to succeed, it must be embraced as a discipline by the materials science and engineering community

## Slide 48: Materials represents a different class of computational problem
Materials response and behavior involve a multitude of physical phenomena with no single overarching modeling approach.
Capturing the essence of a material requires integration of a wide range of modeling approaches dealing with separate and often competing mechanisms and a wider range of length and time scales.
There are over 160,000 engineering materials!
Casting
Precipitation
Micro porosity
Eutectic Phases
Chemistry
Thermodynamics
n
Solution Treatment
Aging
Heat Treatment
Processing
Microstructure
Properties
High Cycle Fatigue
Low Cycle Fatigue
Yield Strength
Thermal Growth
Integration of knowledge domains is
essential to ICME

## Slide 49
Include a manufacturing process(es), a materials system and an application or set of applications that define the critical set of materials properties and geometries
Examples of FEPs
  Lightweight, blast resistant titanium structures
  Superalloy turbine disks for aeropropulsion
  Low cost silicon solar cells
$10-40M per FEP (3-5 year funding)
Prioritize modeling, experimental, data issues to be tackled
Provide a framework for assembly of multidisciplinary teams
Provide near-term payoff (and thus increased buy-in & investment)
Serve as the foundation for this emerging discipline
Foundational Engineering Problems

## Slide 50: What are some additional examples of Foundational Engineering Problems?

## Slide 51: Current Status of ICME
ICME in use at many large companies
ICME - Foundational Engineering Problems
  Forged Ni Turbine Disk Residual Stresses (AFRL/RX)
  ICME Methods for Composite Materials (AFRL/RX)
  Next Generation Auto Sheet Steels (DOE-EERE)
  ICME-Enabled Cast Al alloy development (DOE-EERE) – 3 programs!
  ICME-Enabled Cast Fe alloy development (DOE-EERE) – 2 programs!
  LIFT – ICME Projects

## Slide 52: Residual Stress Engineering in Ni Structures Foundational Engineering Problem (FEP)
Bulk Residual Stress
Surface Residual Stress
Residual stress represents pervasive issue to metals industrial base
Significant “tech pull” from OEM designers and materials suppliers
Significant potential impact:
Reduced development time (decades to years)
Reduced component life cycle cost (up to 50%)
Increased efficiency (up to 20% lower weight)
Reduced scrap at production and depot
Life extension of legacy components
Program developing ICME framework for incorporating residual stress in design of nickel structures
Link disparate materials models for optimization
Integrate computational materials modeling into industrial standard design practice
Define path for pervasive infrastructure needs
  Complementary AFRL In-House Research
  Critical fundamental R&D to enhance industrial toolset, conducted by technical experts at AFRL and academia
“….. to accelerate the
development and application of ICME to critical defense platforms.”

## Slide 53: ICME Guided Development of Advanced Cast Aluminum Alloys For Automotive Engine Application
Hotter Engine
Tpeak = 300 °C
75 % of Tmelting
Current alloy < 250 °C
TMF at valve bridge
Other failure
Thermal Efficiency
hth = 1 – Ten / Top
Faster Development
Traditional Alloy Design
10-20 yr
ICME
Integrated Computational Materials Engineering
Virtual Aluminum Casting “From Atom to Engine”
Alloy Design by ICME ?
2-3 yr
From alloy composition to engine component
New Alloy

## Slide 54: Lightweight Innovations for Tomorrow
New Metals National Manufacturing Innovation Institute
Led by UM, Ohio State U & Edison Welding
Over 100 member consortia of industry, academia and national labs
ICME FEPs are a key technology focus for LIFT
Broadening participation in ICME is a key goal
Materials Commons will be LIFT collaboration platform

## Slide 55
Cyberinfrastructure for ICME
To fully reach its potential, ICME requires new advances in networking, computing, and software:
    Curated, repositories for data and material models and simulation tools
    Linkage of application codes with diverse materials modeling tools
    Geographically dispersed collaborative research
    Dispersed computational resources (Grid computing)
Notes: 55

## Slide 56: Lessons Learned from Other Fields ICME Complexity and Magnitude Similar to Bioinformatics
National Center for Biotechnology Information
Tools and linked databases to develop a better understanding of the molecular processes affecting health and disease
Curated Databases
NIH Requirement
Information Infrastructure in other fields have demonstrated the power of sharing information
$$$

## Slide 57: MGI/ICME Information Infrastructure
NIST
UM Materials
Commons
MDF
ChiMAD
/NIST
Dream 3D
ASM/Granta
3D
Materials
Atlas
Georgia
Tech
MatIN
Miss. State U.
EVOCD
$
USAF-
FEPs
NASA
MAPTIS
U. Minn.
KIMM
Duke
AFLOWLIB
LLNL
Materials
Project
MGI/ICME information infrastructure is beginning to appear
Loose “confederation” is starting to form

## Slide 58: Materials Information Infrastructure
SCIENTIFIC WORKFLOW
STANDARDIZE
CURATE
COLLABORATE
PROVENANCE
SHARE
CLOUD SERVICES
NIST/MDCS
Materials Data Facility
EXPERIMENTS
COMPUTATIONS
EXTERNAL SERVICES
ORGANIZE
PUBLISH
Data Curation
Data Storage
Data Mining
Data Processing
Materials Commons

## Slide 59
The Materials Commons
A unique collaborative environment
Seamless part of scientific workflow including provenance
APIs for Autoingest from PRISMS Codes
Collaboration environment
Interoperable part of growing Materials Information Infrastructure
Publically available Summer 2016

## Slide 60
TEM Images
Quantitative Characteristics
Phase Field Simulation (using
Experimental info to “Parameterize
Nucleation Kinetics)
Comparing Experiments and Simulation
Library of
Analytical Expressions, e.g.
r3=DϒXct-r03
Inputs from CASM
Nucleation Kinetics
Coarsening
kinetics
The Materials Commons
A Use Case: Precipitate Evolution

## Slide 61: Precipitate Evolution – Future Use of Data In Materials Commons
TEM Images
Characteristics available in images which have not been quantified –
but future researcher may need.

## Slide 62
PRISMS Center – Vision of Success
Quantitative
Structure-Property Relations
Quantitative
Processing-Structure Relations
Chemistry
Thermodynamics
Diffusion
Manufacturing
Process
Simulation
Engineering Product Performance Analysis
Constitutive Models
Process & product optimization
Innovation
PRISMS – extensible scientific core for ICME for structural metals
Provide the capability for rapid insertion of the latest science into the engineering process

## Slide 63
PRISMS Center Integrated Framework Enabling accelerated predictive materials science
EXPERIMENTS
(TEM, APT)
Fourier Space DFT
(e.g. VASP)
EXPERIMENTS (slip,
twinning, crack, etc.)
Real Space DFT
PRISMS-RSDFT
Crystal Plasticity
PRISMS-Plasticity
Statistical Mechanics
CASM
Continuum Plasticity
PRISMS-Plasticity
Phase Diagrams
CASM/CALPHAD
Dislocation Dynamics
LLNL-ParaDIS
Phase Field
PRISMS-PF
Atomistic
LAMMPS

## Slide 64: Materials Genome Initiative
Coordinated Multi-agency effort – DOE, DOD, NSF, NIST with White House OSTP leadership
$150M / year “10 year program”
Essential ingredients
  Collaboration
  Integration of theory,
    simulation and experiments
  Information Infrastructure
  Workforce development
  ICME

## Slide 65: ICME/MGI Historical Highlights
1989
DOE: Advanced Strategic Computing Initiative
NRC: Materials Science & Eng for the 1990s
1995
NRC: The Valley of Death
1999
DARPA-AIM
AFOSR-MEANS
2001
2004
2010
2008
NRC-ICME
2011
ONR-D3D
2009
WTEC-SBES
BES-ASCR
We are at a tipping point!
European Union
Virtual Aluminum Castings
For ICME to succeed, it must be embraced as a discipline by the materials science and engineering community

## Slide 66: Materials Genome Initiative
Coordinated Multi-agency effort – DOE, DOD, NSF, NIST with White House OSTP leadership
$150M / year “10 year program”
Essential ingredients
  Collaboration
  Integration of theory,
    simulation and experiments
  Information Infrastructure
  Workforce development
  ICME

## Slide 67: ICME: Current Status in Education and Professional Societies
Educational Efforts
  ICMEd Short Course
  Northwestern U: ICME Certificate Program
  Mississippi State U: ICME Course
Professional Society Efforts (examples)
  TMS International ICME Congress: 2011, 2013, 2015, 2017
  TMS “How To” Guide for Systematic ICME Implementation & Short Course
    http://www.tms.org/icmestudy/
  AIAA ICME Symposia
  AIAA/ASME/TMS Symposia

## Slide 68: What are some things you can do to embed ICME into your curricula?
68

## Slide 69: Integrating ICME into our curriculum
Develop awareness that ICME is possible and valuable
NAE ICME Study: www nae.edu/19582/Reports/25043.aspx
Use ICME tools as a means to enhance the learning experience within the current curricula (but they’re not available yet as integrated tools…)
Therefore focus on:
  Collaboration & Teamwork
  Integration - computational methods & experiments (labs)
  Linkages between specialty areas
  Linkages between science and engineering (Decision Making) – Cross-Disciplinary Design Courses

## Slide 70: ICME in MSE 420 & MSE 520 Undergraduate & Graduate Level Mechanical Behavior
Include ICME as part of the syllabus & a thread throughout the course
Finite Element Analysis Module
  Lecture 1 – Overview (ICME)
  Lecture 2 – COMSOL Hands-on Demo
  2 Homeworks
Team Projects – Matlab ICME Modules

## Slide 71: ICME in MSE 470 Undergraduate Level Physical Metallurgy
Include ICME as part of the syllabus & a thread throughout the course
ThermoCalc & TC PRISMA Analysis Module
  Lecture 1 – Overview (ICME)
  Lecture 2 – ThermoCalc & TC PRISMA Hands-on Demo
  3 Homeworks
Team Projects – Matlab ICME Modules

## Slide 72: Team Project “Educational Module”
Matlab-based model that describes a microstructure-mechanical property (or in MSE 470 a Processing-Microstructure) relationship
Could be used in an undergraduate project to teach a concept – or as part of a larger ICME educational module.
Deliverables:
Model, Paper and Presentation

## Slide 73: Properties of Particle Strengthened Aluminum
Notes: Maybe run the program here~

## Slide 74: Influence of Alloying Elements on Solidification in Ni-based Superalloys
Alloy Options
Varied: Concentrations, Liquidus Slope, Partition Coefficients
Result: Solidification Temperatures vs. Remained Liquid Fraction for different segregating elements

## Slide 75
Casting
Precipitation
Micro porosity
Eutectic Phases
Chemistry
Thermodynamics/
Kinetics
n
Solution Treatment
Aging
Heat Treatment
Processing
Microstructure
Properties
High Cycle Fatigue
Low Cycle Fatigue
Yield Strength
Thermal Growth
ICME (Cast Aluminum) Processing-Structure-Property Linkages

## Slide 76
Casting
Precipitation
Micro porosity
Eutectic Phases
Chemistry
Thermodynamics/
Kinetics
n
Solution Treatment
Aging
Heat Treatment
Processing
Microstructure
Properties
High Cycle Fatigue
Low Cycle Fatigue
Yield Strength
Thermal Growth
Curriculum Linkages

## Slide 77
Casting
Precipitation
Micro porosity
Eutectic Phases
Chemistry
Thermodynamics/
Kinetics
n
Solution Treatment
Aging
Heat Treatment
Processing
Microstructure
Properties
High Cycle Fatigue
Low Cycle Fatigue
Yield Strength
Thermal Growth
Curriculum Linkages
Thermo/Kinetics
Materials Processing
Physical Metallurgy
Mechanical Behavior

## Slide 78: SUMMARY
Integrated Computational Materials Engineering (ICME) offers a means to link:
  Manufacturing, materials and product development
  Engineering and scientific disciplines
  Information across knowledge domain
Virtual Aluminum Castings is an example
  integrated, comprehensive suite of CAE tools that capture extensive expertise in cast aluminum processing, metallurgy & design and provides it to a global engineering workforce.
ICME is an essential ingredient of the Materials Genome Initiative (MGI) and the Next Big Thing in Structural Materials
For the transformational benefits of ICME and MGI to be realized - educators will play a central and critical role.